Data Sheet  	 IN-2FIBER

CPET 110 tex yarn

# H-[C10H8O4]-n=60–120 OH

Each 110 tex  IN-2FIBER  consists of 192 continuous filaments of highly oriented polyethylene terephthalate with multi-matrix compatible sizing.

CPET fiber is a high performance, low cost Thermoplastic yarn optimized for FRP applications

Key properties are low density (1.3) and high strength

| ITEM | UNIT | DATA (Average) | REMARK |
| --- | --- | --- | --- |
| Linear density | Denier - Tex | 1000 - 110 | +/-5% |
| Strength at break | N | 105 |  |
| Elongation at break | % | 11 |  |
| Tenacity | cN/tex | 93 |  |
| Melting Point | °C | 257 |  |

* Test condition : 20±2°C, 65±2% R.H

* Specimen aged 24hrs under 20°C, 65% R.H before test.

* Tensile testing is performed at a yarn twist of 80 TPM.

* Test methods are based on ASTM D-885, ENC standard.