# SPECIFICATION  E GLASS  MARBLES

E Glass marbles are manufactured for the production of glass fiber reinforcement.

1  CHEMICAL PROPERTIES OF E-GLASS (%)

Components				Value	            		        Tolerances

SiO2					54.10				±0.5

Al2O3					14.60				±0.4

CaO					16.60				±0.3

B203				 	  8.80				±0.5

MgO					  4.60				±0.3

Na2O + K2O	            		        					< 0.7

Fe2O3									< 0.5

R2O									< 0.8

Quality Control plan of E glass marbles : internal QP

# PHYSICAL PROPERTIES

-    Diameter (mm) : 				19.50				±1.00

- Non standard marbles :

Broken marbles, small (12g), big (>15g), oval				< 1 / 5000 marbles

## 4     PACKAGING

- Description : 1,000 kg big bags

- Big bag is made of woven polypropylen cloth doubled with PE bag

- Dimensions :  L=900 x l=900 x h=700mm

- Pallet dimension :  L=1150 x l=1150 x h=700mm

## STORAGE

E-glass marbles should be stored in their original packaging, in a dry and dust-free place.