###### NEEDLE MAT

### applications

- this product has been designed for a wide range of processes, such as hand lay up, Pultrusion, winding, GMT, RTM, …

- recommended for FRP products, such as shipbuilding industry, automotive, leisure industry, …

### spEcifications

| Product | Needle combination mat |
| --- | --- |
| Mass (g/m2) | 600±20 |
| Thickness(mm) | 0.78 |
| Structure | needle |
| Sizing | Silane |
| Fabric | yarn (tex) | Warp | 66tex×4×2 |
|  |  | weft | 66tex×3×2 |
|  | Density (ends/cm) | Warp | 3.6 |
|  |  | Weft | 2.8 |
|  |  | Mass (g/m2) | 300 |
| Chopped strand yarn | Mass (g/m2) | 300 |
| Tensile Strength (N/50mm) | Warp | 900 |
|  | Weft | 450 |

#### STORAGE

FRP’s Powder Mats should be stored dry in their original packaging (contracted PE foil and cardboard box). Storage temperature : between 10 and + 35 °C – Relative humidity : between 35 and 85 %.

FRP Services Europe reserves the right to change the information given herein without prior notice. We believe this information to be reliable, but do not guarantee its applicability to the user’s process or assume liability for occurrence arising out of its use. The user, by accepting products described herein

agrees to be responsible for thoroughly testing any application before committing to production.		            	      MAY 2005