###### WOLLASTONITE

### PROPERTIES

| Component | Weight % |
| --- | --- |
| CaO | 46.70 |
| SiO2 | 52.20 |
| Fe2O3 | 0.15 |
| Al2O3 | 0.25 |
| MgO | 0.20 |
| Loss of Ignition | 0.50 |

Wollastonites are acicular mineral products milled to various morphologies and bulk densities. These products can be surface treated to enhance performance in thermoset and thermoplastic resins.

They increase mechanical properties (tensile, flexural, impact) and minimize distorsion at elevated temperatures, improve dimensional stability and provide low moisture absorption.

### spécifications

| Ref. | Average Diameter (microns) | Average Aspect Ratio | Loose Bulk Density (g/cc) | Tapped Bulk (g/cc) | Appearance |
| --- | --- | --- | --- | --- | --- |
| 400U | 4.5 | 7.5 | 0.65 | 0.90 | Powder |
| 400S | 4.5 | 7.5 | 0.67 | 0.95 | Powder |
| 400H | 4.5 | 7.5 | 0.69 | 1.00 | Powder |
| 520U | 5 | 20 | 0.25 | 0.43 | Fiber |
| 520S | 5 | 20 | 0.32 | 0.50 | Fiber |
| 520H | 5 | 20 | 0.37 | 0.59 | Fiber |
| 720U | 5.5 | 20 | 0.32 | 0.60 | Fiber |
| 720S | properties to be determined |
| 720H | 5.5 | 20 | 0.38 | 0.57 | Fiber |
| 800U | 3 | 9 | 0.46 | 0.65 | Powder |
| 800S | 3 | 9 | 0.49 | 0.66 | Powder |
| 800H | 3 | 9 | 0.61 | 0.81 | Powder |
| 905U | 9 | 5 | 0.72 | 1.10 | Powder |
| 905S | 9 | 5 | 0.76 | 1.08 | Powder |
| 905H | properties to be determined |
| 915U | 9 | 15 | 0.50 | 0.83 | Fiber |
| 915S | 9 | 15 | 0.50 | 0.85 | Fiber |
| 915H | 9 | 15 | 0.67 | 0.96 | Fiber |
| 1515U | 15 | 15 | 0.66 | 1.15 | Fiber |
| 1515S | 15 | 15 | 0.58 | 0.97 | Fiber |
| 1515H | properties to be determined |

U=Unsized / S=Amino Silane / H=Hydrophobic / E=Epoxy surface treatments

FRP Services Europe reserve the right to change the information given herein without prior notice. We believe this information to be reliable

But we do not guarantee its applicability to the user’s process or assume liability for occurrence arising out of its use. The user, by accepting

Products described herein, agrees to be responsible for thoroughly testing any application before committing to production.