BFR-711

Product description: BAS-DELTA 117 (13 / 17 my)

Available lengths: 3mm / 6mm / 12mm

Fiber specifications:

BFR-711 is a basalt chopped strand.

This product is coated with a silane-based sizing agent which is designed for compatibility with UP and acrylic resins.

BFR-711 has excellent resin wetting and fiber dispersion.

It is designed for application in panels. Basalt fiber can prolong its life, can improve its performance and can reduce the cost of the project, so it has a strong commercial value. This paper focuses on the short shear basalt fiber reinforced cement mix.

The product is added to the cement mix to improve the mechanical properties and service performance of the surface.

The addition of basalt fiber in the cement mix can improve fracture resistance and anti-ageing crack resistance to significantly extend the service life of the concrete artefact.

Product characteristics:

- Excellent mechanical property.

- Good static control and cuttability.

- Fast external wetting.

- Exceptional dispersion.

- Good stability at high temperatures.

- Good crack resistance at low temperatures.

Functional indicators:

|  | Unit of measurement | Technical specifications |
| --- | --- | --- |
| Thermal conductivity | W / (m · K) | 0.030 - 0.038 |
| Volume resistance | Ω · m | 1 * 10 ^ 12 |
| Chemical composition: total iron oxides | % | ≥ 7.0 |

Technical data sheet:

|  | Unit of measurement | Technical indicators | Test method |
| --- | --- | --- | --- |
| Tensile strength of immersed yarns | MPa | 17 my = 2400 13 my = 2500 | GB / T 20310 |
| Fracture resistance | N/Tex | 17 my: ≥ 0,4 13 my: ≥ 0,5 | GB / T 7690.3 |
| Elongation at break | % | ≤ 3.1 | GB / T 7690.3 |
| Water content | % | ≤ 0.1 | GB / T 9914.1 |
| Presence of fuel content | % | ≤ 0.5 | GB / T 9914.2 |
| Density | g/cm3 | 2.6 - 2.7 | ISO 1183-1 |
| Oil absorption | % | ≥50 | - |
| Moisture content | % | ≤0.2 | - |
| Flammability | - | None | - |
| Heat resistance | % | ≥85 | - |
| Elasticity | GPa | ≥80 |  |

Packaging:

BFR-711 is available packed in 20 kg plastic bags in oktabin or pallets, or other packaging on request.

Basalt fiber is a brittle inorganic material, bending and contact with rough surfaces should be avoided and unnecessary friction reduced.

Storage:

BFR-711 should be stored in a dry, cool, moisture-proof area and should remain in its original packaging until used.

Validity:

BFR-711 remains valid for up to 12 months from the date of leaving the factory.

Technical parameters:

| Linear density (%) | Moisture content (%) | Size content (%) | Rigidity (mm) |
| --- | --- | --- | --- |
| ISO 1889 | ISO 3344 | ISO 1887 | ISO 3375 |
| ± 5 | ≤ 0.10 | 0.6 ± 0.15 | ≥ 105 |

Data parameters:

| Type of sizing | Silane |
| --- | --- |
| Filament (my) | 13 / 17 |